## Slide 1: The Basics of Automotive Surface Engineering by Isotropic Superfinishing
Bill Nebiolo
Sr. Tech. Acct. Eng’r; Midwest U.S.A.
Email: bnebiolo@remchem.com
Website: www.remchem.com
© 2015 REM Chemicals, Inc. All rights reserved REM, ISF and REM Surface Engineering are registered trademarks of REM Chemicals, Inc. This presentation contains confidential and proprietary information of REM Chemicals, Inc., and may not be reproduced or redistributed without the express written consent of REM Chemicals, Inc.
REM®, ISF®, FERROMIL®, & MAGALLOY® are a registered trademarks of REM Chemicals Inc.

## Slide 2: Traditional Processing; Grinding or Lapping
© 2015 REM Chemicals, Inc.
Post Heat Treatment Grinding
Post heat treat
grinding removes
quench distortion

## Slide 3: Traditional Ground Finish; Part is ready for installation
© 2015 REM Chemicals, Inc.
Beveled Spur Gear After Tooth Grinding
Note; tooth
showing
grind lines

## Slide 4: Traditional Ground Surface; Unidirectional & Failure Initiative
© 2015 REM Chemicals, Inc.
Magnified View of Ground Tooth Flank

## Slide 5: As Ground Opposing Surfaces; Contact Inefficiency
© 2015 REM Chemicals, Inc.
The two opposing as-ground tooth flank surfaces during the initial break-in phase
Gear mesh compressive stress on opposing tooth flanks is concentrated into just a few asperity-to-asperity contact locations
Initial contact during break-in period is asperity to asperity

## Slide 6: ISF Processed Part; Controlled Asperity Planarization
© 2015 REM Chemicals, Inc.
Beveled Spur Gear After ISF Processing
Same gear tooth after ISF, surface asperities planarized

## Slide 7: ISF Surface; Non-directional & Textured for Lube Retention
© 2015 REM Chemicals, Inc.
REM ISF Isotropic Super Finish Enhanced Surface Texture

## Slide 8: The ISF Process; Asperities Planarized
© 2015 REM Chemicals, Inc.
Two REM ISF gear tooth flanks during initial contact loading
Gear mesh compressive stress on opposing tooth flanks is much lower because it is now diffused across a larger surface area.
Asperities have undergone controlled leveling

## Slide 9: The ISF Process; Processing Equipment Traditional
© 2015 REM Chemicals, Inc.
ISF is Generated in a Vibratory Bowl or a Vibratory Tub

## Slide 10: The ISF Process; Processing Equipment Rapid ISF
© 2015 REM Chemicals, Inc.
Rapid ISF
Drag Finisher
Combine drag finisher with chemical accelerator to ISF gearsets in just one minute

## Slide 11: Non-Abrasive Media for Controlled Asperity Removal
© 2015 REM Chemicals, Inc.
Traditional Abrasive Vibe Media
REM ISF Media
Abrasive Angle Cut Triangles Note: Aluminum Oxide Grit
High Temperature Fired Vitrified, Non-Abrasive High Density Media

## Slide 12: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
7x Photomicrograph of as-ground tooth flank
Ground starting condition
Ra = 55 µin. (1.37 µm)
Rmax = 470 µin. (11.8 µm)
Profilometry Trace

## Slide 13: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
The ISF Process
ISF® chemistry forms a soft surface conversion coating.
Coating is softer than the part upon which it has formed.

## Slide 14: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
The ISF Process
Media wipes soft conversion coating from the tops of the asperities and asperities begin to planarize

## Slide 15: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
7x Photomicrograph after a short period of time
Profilometry Trace shows partial asperity planarization
Partial asperity planarization
Ra = 23 µin. (0.57 µm)
Rmax = 187 µin. (4.67 µm)

## Slide 16: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
The ISF Process
Coating reforms on partially planarized asperities and additional media wiping continues planarization

## Slide 17: The ISF Process; Planarization Mechanism
© 2015 REM Chemicals, Inc.
7x photomicrograph a little while longer
Significant asperity planarization
Ra = 12 µin. (0.3 µm)
Rmax = 95 µin. (2.4 µm)
Profilometry tracing shows substantially planarized asperities

## Slide 18: ISF Processing; Burnish to produce clean final surface
© 2015 REM Chemicals, Inc.
The ISF Process
When desired Ra is achieved a soap burnishing step removes the ISF coating

## Slide 19: ISF Processing; the Planarization Mechanism
ISF chemistry forms a soft conversion coating
ISF HDNA media generates final micro-texture surface
The as-ground surface becomes an ISF surface

## Slide 20: This ISF Process; Final Finish
© 2015 REM Chemicals, Inc.
The ISF Process
Final Profilometry Trace
The final ISF finish
Ra = 2.49 µinches
Rmax = 0.098 µm

## Slide 21: ISF Advantages “Eliminate Component Break-in”
© 2015 REM Chemicals, Inc.
Schematic Diagram; Block-on-Ring Test
Block-on-Ring Test
Block held on rotating
ring under constant load
of 8 lbs.
Temperature of lubricant
bath monitored during
test

## Slide 22
© 2015 REM Chemicals, Inc.
Block-on-Ring Specimen Preparation
Control Ground Specimen
ISF Prepared Specimen
Sample I.D. | Surface Ra Value
Control Sample Ground Block #1 | 25 μin. or 0.64 μm
Control Sample Ground Block #2 | 29 μin. or 0.75 μm
ISF Prepared Block Specimen #1 | 2.3 μin or 0.06 μm
ISF Prepared Block Specimen #2 | 5.1 μin or 0.13 μm
ISF Advantages “Eliminate Component Break-in”

## Slide 23: No Component Break-in; Parts Run Cooler
© 2015 REM Chemicals, Inc.
Block-on-Ring Test Results
Traditional Ground Block
Break-in temperature spike
Higher final operating temp.
ISF Prepared Block
No break-in temp spike
Lower final operating temp.

## Slide 24: Reducing Parasitic Friction; Parts Run Smoother
© 2015 REM Chemicals, Inc.
Reduction of Parasitic Friction
Full ISF Refined Bearing set ran 34º F cooler at highest loading

## Slide 25: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
Schematic of Rolling/Sliding Contact (R/SCF) Fatigue Test Rig
Test Specifics
43% negative slide
on specimen
Test loading at 400,
425 & 450 KSI
Successful test run
= 20 million cycles

## Slide 26: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Test Pin & Load Roller
Specimen Specifics
SAE 9310H
Carburized Rc 60-65
Ra = 15μin/0.6μm
1” diameter pin
5” diameter roller

## Slide 27: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Sample Preparation Parameters
Sample Identification | Test Component Surface Ra Value
Ground Components Control Standard | 15 μinches or 0.38 μm
ISF Prepared Components | 1.5 μinches or 0.04 μm

## Slide 28: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Test Contact Fatigue Pitting Results
Ground to Ra = 16μin Control Standard Samples
Sample I.D. | Contact Stress Load in ksi | Test Duration in million cycles | Failure Mode
#1 | 400 | 3.6 | Pitted
#2 | 400 | 4.2 | Pitted
#3 | 400 | 3.5 | Pitted

## Slide 29: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Test
Photographic Results
Photo Shows
Pitting Failure of 1” Ground Control Standard Specimen after 3.5 million cycles @ 400 KSI Contact Stress Loading

## Slide 30: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Test Results ISF Prepared Specimens
Sample I.D. | Contact Stress Loading in ksi | Duration in millions of cycles | Failure Mode
#1 | 400 | 20.0 | No Failure
 | 425 | 20.0 | 
 | 450 | 22.4 | 
Cumulative Result | 400-450 | 62.4 | No Failure
#2 | 400 | 5.0* | No Failure
 | 425 | 5.0* | 
 | 450 | 20.0 | 
Cumulative Result | 400-450 | 30.0 | No Failure

## Slide 31: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
R/SCF Test
Photographic Results
Photo Shows
1” REM ISF Specimen after
62.4 million cycles @ 400,
425 & 450 KSI Contact Stress Loading

## Slide 32: ISF Advantages; “Virtual Elimination of Contact Fatigue”
© 2015 REM Chemicals, Inc.
Virtual Elimination of Contact Fatigue
Combined R/SCF Test Photographic Results
Top Photo
Standard Ground Specimen
after 3.5 million cycles
Pitting Failure
Bottom Photo
REM ISF Specimen
after 62.4 million cycles
No Pitting Failure

## Slide 33: ISF Advantages; Benefits of an ISF Surface
© 2015 REM Chemicals, Inc.
Conclusion; Benefits of ISF
Eliminate Component Break-on with controlled asperity planarization
Eliminate metal debris in the lubricant stream
More efficient metal-to-metal surface contact increases power density
Compressive contact stresses are diffused over a larger area
Reduction of parasitic, frictional heat generation. Parts run cooler
More efficient transfer of energy at metal-to-metal contact surfaces
Reduction of contact fatigue failure
Improved surface quality reduces onset of corrosion
Improved surface quality electroplates more efficiently

## Slide 34: ISF Advantages; “Reduction of Surface Contact Stress”
© 2015 REM Chemicals, Inc.
REM Surface Engineering
www.remchem.com
Surface Engineering Specialists
An ISO9001:2015/AS9100 Rev D Certified Company With Offices In:
Manufacturing and JSS in Southington, CT
Serial Production Volume JSS in Merrillville, IN
Engineering, R&D, Manuf. and JSS in Brenham, TX
Corporate Offices in Austin, TX
Manufacturing and JSS in St. Neots, Cambridgeshire, U.K.